## Slide 1: PFEM-based 2D phase change simulation tool applied to laser spot welding
Billy-Joe Bobach1, billy-joe.bobach@uliege.be Roman Boman1 Prof. Diego Celentano2 Prof. Vincent Terrapon1 Prof. Jean-Philippe Ponthot1
1Uliège Belgium; 2PUC Santiago de Chile
funded by a F.N.R.S. FRIA research grant

## Slide 2
Common characteristics
  Localized/concentrated heat source
  Melting & resolidification
  Melt pool unknown & evolving
Additive Manufacturing and related manufacturing processes
Laser
Powder bed
Part
Example: Selective Laser Melting (SLM)
Example: Friction Melt Bonding (FMB)
van der Rest, Jacques, Simar, Scripta Materialia 2014
and many more...
Future work in our lab
Presented today: Laser spot welding  same characteristics, but simpler

## Slide 3
Heat source
Heat transfer
Melt pool fluid dynamics
Melting & solidification
Residual stresses and distortion after cooling
transient & coupled
unknown & evolving Interfaces
multi-physics simulation at meso-scale
Solid
Liquid
Laser (stationary for spot welding)
Solid
Liquid

## Slide 4: Proposed approach
Particle finite element method (PFEM)
First developments: Idelsohn et al., Int. J. Num. Methods Eng., 2004
Comprehensive review: Cremonesi et al., Arch. Comput. Methods Eng., 2020
Robust as FEM
Flexible as a particle method
Well suited for free surface
Not been used in this context

## Slide 5
PFEM explained: example dam break
Delaunay
Nodes
-shape
FEM
deform
FEM
deform
Meshing
Lagrangian Finite elements
+
Fast & smart remeshing
+
Solution () stored at the nodes
Large deformation
No mesh distortion
Solid & Fluid
Evolving boundaries captured
  Free surface
  Splashing
Delaunay
+
-shape

## Slide 6
M. Cerquaglia, Doctoral thesis ULiège, 2019
PFEM explained: example dam break

## Slide 7: Equations to solve
Liquid, mushy & solid regions solved on same mesh using:
Navier-Stokes equations (NSE)
  Lagrangian formulation
Heat equation
Surface tension
flow resistance
of mushy zone (and solid)
Laser heat source
Latent heat absorption

## Slide 8: Equations to solve
Momentum equation for newtonian fluids
Surface tension
Resulting surface force term
Normal force
Tangential marangoni force
Note: Marangoni coefficient usually negative  surface force away from heat source
= curvature
= outward normal
= surface tension at = Marangoni coefficient
Surface tension term

## Slide 9: Equations to solve
Momentum equation for Newtonian fluids
Liquid fraction
Mushy zone flow resistance term
Carman-Kozeny eq.
Chosen coefficient
Avoid div. by 0
Reduces momentum, as (effectively freezing the solid)
Note: dyn. viscosity for solid and fluid
1
0
Solidification flow resistance tension term

## Slide 10: Equations to solve
Heat equation
Volume heat source
Heat source term

## Slide 11: Equations to solve
Heat equation
Latent heat absoprtion
  Highly non-linear
as
0
1
0
Improve stability using regularization
would be +inf
Can become very large
Latent heat term

## Slide 12: Equations to solve
Heat equation
Latent heat absoprtion
  Modifies jacobian of non-linear algorithm (e.g. Newton-Raphson‘s tangent stiffness matrix), restores continuity (), defined at
  Does not modify residual  result is correct, if converged
Regularization
Cubic polynomial
1
0
1
0
Latent heat term

## Slide 13: Numerics
time integration: Backward Euler fully implicit
solution scheme: staggered, weakly coupled
non-linear algo: Newton-Raphson for heat eq. Picard iterations for NSE + line search algo (faster convergence)
element type: linear triangles (3 nodes) 3 Gauss points (required near sym. axis) Pressure-Stabilizing Petrov-Galerkin
see e.g. Cerquaglia, M., PhD thesis ULiège, 2019
Heat eq.
N-S eq.
Converged?
Converged?
one time step
iterate
iterate

## Slide 14: Adaptive mesh refinement (using simple example: imposed T field with a gradient)
PFEM remeshes every time step
Nodes can be inserted or removed (Delaunay does the rest)
When and where to add/remove nodes can be based on solution
We refine, where
  is high
  is high
Note: based on work by R. Falla, Uliège. Paper not yet submitted

## Slide 15: Laser Spot welding test case
Steel
No atmosphere modeled
Total time: 5s
Simulations by Saldi, Z., PhD thesis TU Delft, 2012
Experiments by Pitscheneder et al., Supplement to the welding Journal, 1996

## Slide 16: Heat source
Steel
Total power is constant in time
Source term is only applied inside the box
Volume inside box is sampled (possible deformation of surface)
Power density is calculated:
Note:
Power density is constant in space inside box
No attenuation in depth (e.g. Beer-Lambert)
No variation over radius (e.g. Gaussian distr.)

## Slide 17: Simulation setup
Use axisymmetry
Adiabatic, rigid
Adiabatic rigid
axisymmetry
Adiabatic, free surface
Volume heat source
Total time: 5s Time step: 1ms

## Slide 18: Properties
Steel
quantity | symbol | value | unit
Density |  |  | 
Dyn. viscosity |  |  | 
Conductivity |  |  | 
Specific heat capacity |  |  | 
Melting point |  |  | 
Latent heat |  |  | 
quantity | symbol | value | unit
Density |  |  | 
Dyn. viscosity |  |  | 
Conductivity |  |  | 
Specific heat capacity |  |  | 
Melting point |  |  | 
Latent heat |  |  | 

## Slide 19: Properties
Note:
Surface tension normal force is neglected in this case (following reference test case by Saldi)

## Slide 20: Initial mesh
Coarse:
Fine:
Simulation results will show this top left corner!

## Slide 21
Liquid
Mushy
Solid
No flow

## Slide 22
Melting front advancing
and fine mesh follows
Liquified portion of surface is deforming under Marangoni force

## Slide 23
Liquid material builds up at the free surface and freezes again at melting front
Convective flow sets in, driven by Marangoni force at surface

## Slide 24
With increasing velocity, the refinement sets in
Melting front advancement slows down significantly
Strong circulation, at the surface, where is largest

## Slide 25: Comparison with literature
Saldi, 2012 (Simulation)
Temperature field
Velocity vectors
After 5s

## Slide 26: Comparison with literature
Saldi, 2012 (Simulation)
Temperature field
Velocity vectors
After 5s
1620
1700
1800
1900
2000

## Slide 27: Comparison with literature
Saldi, 2012 (Simulation)
Velocity vectors
After 5s
Note: deformation of free surface

## Slide 28
Saldi, 2012 (Simulation) Pitscheneder et al. 1996 (Exp.)
After 5s
No deformation of free surface
Comparison with literature
deformation of free surface

## Slide 29
Saldi, 2012 (Simulation) Pitscheneder et al. 1996 (Exp.)
After 5s
Comparison with literature
deformation of free surface
deformation of free surface, but different than experiment

## Slide 30
Comparison with literature
Observations:
Max. temperature is higher than expected
Melt pool dimensions are larger than expected
Max. velocity is smaller than expected
Surface deformation is different than in experiment
Possible explanation for discrepancies:
Input power too high? No, verified
More time has passed? No, same time
Boundary conditions wrong? possible, no problem found yet
Material properties wrong? possible, no problem found yet
Deformed surface affecting result? possible, but not sure how
Bug in the code? very possible, all features are validated on their own, but not necessarily in combination
 More work needed

## Slide 31: Conclusion
These particular results are not reliable, but
PFEM handles well
  free surface deformation
  phase change with latent heat
  surface tension & Marangoni effect
  adaptive mesh refinement

## Slide 32: Future work
Explain different results
Compare with more literature cases
Add more physics for more advanced cases
  Recoil pressure
  Evaporative cooling
More realistic heat source (Gaussian distr. over + Beer-Lambert law over )
Add a powder phase (for additive manufacturing, e.g. SLM)
  As continuous phase (simple, but suitable for ceramics, not metals)
  Incl. Effective heat conduction
Implementation of elasto-plastic solid